## Slide 1
SSimulation of a flip-chip architecture
of superconducting quantum processor
Simulation
Distance dependence of parameters
qubit
Qchip ground
qubit
Qchip ground
qubit
Qchip ground
Flip chip qubit :
Capacitive effect takes over
d C  Ec
qubit
Qchip ground
qubit
Qchip ground
qubit
Qchip ground
Coupling strength:
Capacitive effect takes over
d C 
CPW
Qchip ground
CPW
Qchip ground
CPW
Qchip ground
Flip chip resonator :
Inductive effect takes over
Effective cavity change(2d  3d cavity)
Introduction
What & Why Flip-Chip
D. I. Schuster et at.. 2019.
Sandoko Kosen et al 2021.
Bottom, Top chip can contain any component
- Various chip size
- Inductive, Capacitive, Galvanic coupling
- Indium bump bonding/ PR Adhesion
 Distribute components into different layers
 Independent chip fabrication  high coherence qubit layer + dense wiring layer
C. R. Conner et al. . 2021.
Planar chip, Problem
Every component on same plane
Superconducting qubit system is getting bigger and more complex
 When the chip becomes complex with more components  difficult wiring, qubit decoherence
SKKU, 20qubit
Google 9qubit
Circuit QED – Resonator, Transmon, coupling strength
Transmon : Non-linear inductor (Josephson Junction)+ big shunt Capacitor  anharmonic quantum oscillator
Resonator : Linear inductor + capacitor  harmonic quantum oscillator
Coupling strength : determined by capacitive coupling between Transmon and Resonator
Distance | Qubit (GHz) | Resonator (GHz) | Coupling g (MHz)
5um | 5.42 | 7.58 | 153
6um | 5.69 | 7.36 | 133
7um | 5.88 | 7.20 | 115
8um | 6.03 | 7.10 | 99
9um | 6.12 | 7.01 | 95
Qubit (GHz) |  | Resonator(GHz) | 
Bump O | Bump X | Bump O | Bump X
5.69 | 5.30 | 7.36 | 6.18
5.88( | 5.56( | 7.20( | 6.45(
6.03( | 5.60( | 7.10( | 6.37(
Qubit (GHz) |  | Resonator(GHz) | 
Bump O | Bump X | Bump O | Bump X
5.69 | 5.30 | 7.36 | 6.18
Jeongwon Kim1, Hwan-Seop Yeo1, Seungwook Woo1, Youngdu Kim1, Beomgyu Choi1, and Yonuk Chong1,*
1SKKU Advanced Institute of Nanotechnology and Department of Nano Engineering, Suwon, 16419, Republic of Korea E-mail : bicycle315@skku.edu
Targeting planar chip parameters in flip-chip
Targeting within
Qubit:2.1%, Resonator : 2.7% g: 3.4%
Distance dependence of parameters
Bump effect
Result
Conclusion & Future plan
Conclusion1 : Established simulation tools for flip chip architecture
Conclusion 2 : Can target the planar chip’s parameters in flip chip architecture
Plan1 : Simulate bigger scale flip chip including qubit couplers
Plan2 : Study and optimize the bump condition
Simulation Tool
Qiskit-Metal
Ansys HFSS,Q3D
 | Qubit Frequency(GHz) | Resonator frequency(GHz) | Coupling strength (MHz)
Planar | 6.01 | 7.00 | 111
7um Flipchip-planar design | 5.09 | 7.33 | 39
7um Flipchip- Modified design | 5.88 | 7.20 | 115
Design modification to target the parameters
Resonator length
Coupler area
Transmon area
Couper, Transmon coupling area
Siddiqi, 8qubit
Chip Parameter
Chips
Qubit chip (components: qubit) : 2mm*2mm
Control chip (components : resonator, feedline, launchpad) : 3mm*3mm
2. Inter-chip distance (5~10um) - at least 2um
CPW impedance change by the Q-chip ground plane (if d<2um)  smooth impedance transition under the edge of the top chip
- less than 10um
 Capacitive effect dramatically depend on the distance
3. Bump condition
- 50~100/  180
- 100~200 spacing 100um
- Width=1.5*height
Planar
2D
Resonator
CPW
Qchip ground
CPW
Flipchip
3D
Cavity
Qubit chip
Control chip